NALYSIS SCIENTIFIC LTD

Rocklands 9 Rockcliffe Villas Bacup Lancs OL13 8JG UK

Tel: 01706 871700 www.analysis-scientific.co.uk

Email: brenda.peters@analysis-scientific.co.uk

Report prepared for: Little Greene Paint Company

Subject: Toy Regulations EN71-3:2019+ A1:2021

Intelligent ASP (AD/091120)

Report no. 91003/21

Date: 22 February 2021

Specification: BS EN 71-3:2019+A1:2021

Acid extraction method was used and migration elements content were determined by Inductively Coupled Plasma-ICP-MS

CONCLUSION: The results of the tests carried out MEET the requirements of the

Standard Toy Regulations EN71-3:2019+A1:2021 Category II Liquid/Sticky

| Element | EN71-3: 2019 Limits Category II | Intelligent ASP (AD/091120) |
| --- | --- | --- |
|  | mg/kg |  |
| Aluminium | 1406 | 953.3 |
| Antimony | 11.3 | <0.2 |
| Arsenic | 0.9 | <0.1 |
| Barium | 375 | <100 |
| Boron | 300 | <100 |
| Cadmium | 0.3 | <0.125 |
| Chromium (III) | 9.4 | <0.004 |
| Chromium (VI) | 0.005 | <0.004 |
| Cobalt | 2.6 | <0.5 |
| Copper | 156 | <50 |
| Lead | 0.5 | 0.21 |
| Manganese | 300 | <100 |
| Mercury | 1.9 | <0.05 |
| Nickel | 18.8 | <6 |
| Selenium | 9.4 | <3 |
| Strontium | 1125 | <250 |
| Tin | 3750 | <0.2 |
| Organic Tin | 0.2 | <0.2 |
| Zinc | 938 | 305.4 |

Brenda Peters FTSC FIMF FICorr CSci

Company No 11282709

VAT No GB508 2760 50