NALYSIS SCIENTIFIC LTD

Rocklands 9 Rockcliffe Villas Bacup Lancs OL13 8JG UK

Tel: 01706 871700 www.analysis-scientific.co.uk

Email: brenda.peters@analysis-scientific.co.uk

Report prepared for: Little Greene Paint Company

Subject: Toy Regulations EN71-3:2019 + A1:2021

Intelligent Matt

DP17H Batch no. 043-048

Report no. 107781/22

Date: 15 August 2022

Specification: BS EN 71-3:2019+A12019

Acid extraction method was used and migration elements content were determined by Inductively Coupled Plasma-ICP-MS

CONCLUSION: The results of the tests carried out PASSES the requirements of the

Standard Toy Regulations EN71-3:2019+A1-2021 Category III scraped off toy material e.g. plastic, paint, coatings, textiles

Brenda Peters FTSC FIMF FICorr CSci

Company No 11282709

VAT No GB508 2760 50

| Element | EN71-3: 2019+A13032 Limits Category II | Architects Matt Emulsion DP17H Batch No.043-040B |
| --- | --- | --- |
|  | mg/kg | mg/kg |
| Aluminium | 28130 | 3216 |
| Antimony | 560 | <0.2 |
| Arsenic | 47 | <0.1 |
| Barium | 18750 | <100 |
| Boron | 1500 | <100 |
| Cadmium | 17 | <0.125 |
| Chromium (III) | 460 | <0.004 |
| Chromium (VI) | 0.053 | <0.004 |
| Cobalt | 130 | <0.5 |
| Copper | 7700 | <50 |
| Lead | 27 | <0.125 |
| Manganese | 15000 | <100 |
| Mercury | 94 | <0.05 |
| Nickel | 930 | <6 |
| Selenium | 460 | <3 |
| Strontium | 56000 | <250 |
| Tin | 180000 | <0.2 |
| Organic Tin | 12 | <0.2 |
| Zinc | 46000 | 691 |